Electroless and Electrodeposition of Copper and Nickel

Substrates available in our lab:

- Steel

- Brass

- Copper

- ABS (Acrylonitrile butadiene styrene) plastic

General working order instructions:

- All baths are prepared for 50 ml solution.

- Polish the electrode, rinse and dry.

- Weight the electrode before plating.

- Measure the electrode thickness before plating.

- Perform the electroplating process.

- Rinse the electrode after each treatment.

- Dry the coated electrode.

- Weight the electrode after plating.

- Measure the electrode thickness after plating.

- Perform the below mentioned tests (if needed).

Parameters to be considered in the electroplating processes:

| Tests | Electroless | Electrodeposition |
| --- | --- | --- |
| Coating thickness (d), μm | + | + |
| Coating weight (A), gr | + | + |
| Porosity | + | + |
| Adhesion | + | + |
| Grain size (optic microscope) | + | + |
| Quenching | + | + |
| Coating roughness | + | + |
| Amount of precipitate in solution (B), gr | + | - |
| Stability of solution (C), % C=AA+B∗100% | + | - |
| Plot thickness/weight vs. current density/deposition time (4 graphs) | - | + |

Discuss your results in order to answer your research question (research hypothesis).

Porosity test procedure:

  - Prepare the porosity bath as described in the procedure.

  - Place double sheet of paper on the table.

  - Place two glass slides on top of the paper.

  - Put filter paper on each slide.

  - Put some of the porosity solution on top of one filter paper with plastic pipette.

  - Place your electrode on the wet filter paper, and then pour some more porosity solution on top of the electrode.

  - Place the other filter paper on top, make sure it is wet (if not add some more solution).

  - Place the second glass slide on the top and wait 20 minutes.

Experiment  1 - Electroless deposition of Ni

Experiment conditions:

| Bath description (prepare 50 ml baths) | Operating parameters | Composition of the solution | Concent. of the compounds |  | Notes |
| --- | --- | --- | --- | --- | --- |
|  |  |  | g/L | ml/L |  |
| 1. Degreasing | Temp - RT | Na2CO3 | 15 |  |  |
|  | Time – 5min | Na3PO4*12H2O | 35 |  |  |
|  |  | NaOH | 35 |  |  |
| 2. **Etching | Temp - RT | - H2SO4 conc. |  | 1000 | for steel/ABS electrode |
|  | a. Time – 5min | K2Cr2O7 | 50 |  | Decant the solution |
|  | b. Time – 1 min | - HNO3 1M |  |  | For copper electrode |
|  | c. Time – 5 min | - HNO3 1M |  |  | For brass electrode |
| 3. *Sensibilization | Temp - RT | SnCl2*2H2O | 25 |  | Dissolve completely in HCl conc. on heating, then add water |
|  | Time – 5min | HCl conc. |  | 200 |  |
| 4. *Activation | Temp - RT | PdCl2 | 1.5 |  | Dissolve completely in HCl conc. on heating, then add water |
|  | Time – 1min | HCl conc. |  | 20 |  |
| 5. Ni bath | Temp – 70-90 oC | NiSO4•6H2O | 16 |  |  |
|  | Time – 10-30min | Na3C6H5O7•2H2O | 18 |  |  |
|  | pH 9-11 | NH2CSNH2 | 0.001-0.002 |  | Prepare stock solution, then dilute, for example: 10mg/L then dilute by 10 |
|  |  | NH4OH |  |  | Adjust to pH 9-11 |
|  |  | NaH2PO2•H2O | 17 |  | Add just before plating |
| 6. Porosity test | Temp - RT | K3Fe(CN)6 | 10 |  |  |
|  | Time – 5min | NaCl | 20 |  |  |

*Prepare those baths only if needed.

- Experiment suggestion: comparison between electroless and electrodeposition.

** prepare one of three possible etching baths accordingly to the electrode used.

Experiment 2- Electroless deposition of Cu

Experiment conditions:

| Bath description (prepare 50 ml baths) | Operating parameters | Composition of the solution | Concent. of the compounds |  | Notes |
| --- | --- | --- | --- | --- | --- |
|  |  |  | g/L | ml/L |  |
| 1. Degreasing | Temp - RT | Na2CO3 | 15 |  |  |
|  | Time – 5min | Na3PO4*12H2O | 35 |  |  |
|  |  | NaOH | 35 |  |  |
| 2. **Etching | Temp - RT | - H2SO4 conc. |  | 1000 | for steel/ABS electrode |
|  | a. Time – 5min | K2Cr2O7 | 50 |  | Decant the solution |
|  | b. Time – 1 min | - HNO3 1M |  |  | For copper electrode |
|  | c. Time – 5 min | - HNO3 1M |  |  | For brass electrode |
| 3*.Sensibilization | Temp - RT | SnCl2•2H2O | 25 |  | Dissolve completely in HCl conc. on heating, then add water |
|  | Time – 5min | HCl conc. |  | 200 |  |
| 4*. Activation | Temp - RT | PdCl2 | 1.5 |  | Dissolve completely in HCl conc. on heating, then add water |
|  | Time – 1min | HCl conc. |  | 20 |  |
| 5a. Cu bath | Temp - RT | CuSO4•5H2O | 35 |  |  |
| Option A | Time – 5-30min | KNaC4H4O6•4H2O | 150 |  |  |
|  | pH 11-13 | Na2CO3 | 35 |  |  |
|  |  | NaOH |  |  | Prepare 3-6M solution, adjust to pH 11-13 |
|  |  | HCOH (35%) |  | 20 | Add just before plating |
| 5b. Cu bath | Temp - RT | CuSO4•5H2O | 35 |  |  |
| Option B | Time – 5-30min | Na2(EDTA)•2H2O | 60 |  |  |
|  | pH 11-13 | NaOH |  |  | Prepare 3-6M solution, adjust to pH 11-13 |
|  |  | HCOH (35%) |  | 20 | Add just before plating |
| 6. Porosity test | Temp - RT | K3Fe(CN)6 | 10 |  |  |
|  | Time – 20min | NaCl | 20 |  |  |

*Prepare those baths only if needed.

** prepare one of three possible etching baths accordingly to the electrode used.

- Experiment suggestion: comparison between electroless and electrodeposition.

Experiment 3- Electrodeposition of Ni

Experiment conditions:

| Bath description (prepare 50 ml baths) | Operating parameters | Composition of the solution | Concent. of the compounds |  | Notes |
| --- | --- | --- | --- | --- | --- |
|  |  |  | g/L | ml/L |  |
| 1. Degreasing | Temp - RT | Na2CO3 | 15 |  |  |
|  | Time – 5min | Na3PO4*12H2O | 35 |  |  |
|  |  | NaOH | 35 |  |  |
| 2. **Etching | Temp - RT | - H2SO4 conc. |  | 1000 | for steel electrode |
|  | a. Time – 5min | K2Cr2O7 | 50 |  | Decant the solution |
|  | b. Time – 1 min | - HNO3 1M |  |  | For copper electrode |
|  | c. Time – 5 min | - HNO3 1M |  |  | For brass electrode |
| 3. *Sensibilization | Temp - RT | SnCl2*2H2O | 25 |  | Dissolve completely in HCl conc. by heating, then add water |
|  | Time – 5min | HCl conc. |  | 200 |  |
| 4. *Activation | Temp - RT | PdCl2 | 1.5 |  | Dissolve completely in HCl conc. by heating, then add water |
|  | Time – 1min | HCl conc. |  | 20 |  |
| 5a. Ni bath | Temp – 70-90 oC | NiSO4•7H2O | 16 |  |  |
| Option A | Time – 10-30min | NiCl2•6H2O | 3 |  |  |
|  | pH 9-11 | Na3C6H5O7•2H2O | 18 |  |  |
|  | Current density - 50-500 A/m2 | NH4OH |  |  | Adjust to pH 9-11 |
| 5b. Ni bath | Temp – RT | NiSO4•7H2O | 80 |  |  |
| Option B | Time – 5-30min | NiCl2•6H2O | 15 |  |  |
|  | pH 3-5 | H3BO3 | 10 |  |  |
|  | Current density - 50-500 A/m2 | H2SO4 |  |  | Adjust to pH 3-5 |
| 6. Porosity test | Temp - RT | K3Fe(CN)6 | 10 |  |  |
|  | Time – 5min | NaCl | 20 |  |  |

*Prepare those baths only if needed.

** prepare one of three possible etching baths accordingly to the electrode used.

- Experiment suggestion: adding 0.0025-0.05gr of copper impurities to Ni bath.

- Experiment suggestion: comparison between electroless and electrodeposition.

Experiment 4- Electrodeposition of Cu

Experiment conditions:

| Bath description (prepare 50 ml baths) | Operating parameters | Composition of the solution | Concent. of the compounds |  | Notes |
| --- | --- | --- | --- | --- | --- |
|  |  |  | g/L | ml/L |  |
| 1. Degreasing | Temp - RT | Na2CO3 | 15 |  |  |
|  | Time – 5min | Na3PO4*12H2O | 35 |  |  |
|  |  | NaOH | 35 |  |  |
| 2.** Etching | Temp - RT | - H2SO4 conc. |  | 1000 | for steel electrode |
|  | - Time – 5min | K2Cr2O7 | 50 |  | Decant the solution |
|  | b. Time – 1 min | - HNO3 1M |  |  | For copper electrode |
|  | c. Time – 5 min | - HNO3 1M |  |  | For brass electrode |
| 3. *Sensibilization | Temp - RT | SnCl2*2H2O | 25 |  | Dissolve completely in HCl conc. by heating, then add water |
|  | Time – 5min | HCl conc. |  | 200 |  |
| 4. *Activation | Temp - RT | PdCl2 | 1.5 |  | Dissolve completely in HCl conc. by heating, then add water |
|  | Time – 1min | HCl conc. |  | 20 |  |
| 5a. Cu bath | Temp - RT | CuSO4•5H2O | 35 |  |  |
| Option A | Time – 5-30min | KNaC4H4O6•4H2O | 150 |  |  |
|  | pH 11-13 | Na2CO3 | 35 |  |  |
|  | Current density - 50-500 A/m2 | NaOH |  |  | Prepare 3-6M solution, adjust to pH 11-13 |
| 5b. Cu bath | Temp - RT | CuSO4•5H2O | 35 |  |  |
| Option B | Time – 5-30min | Na2(EDTA) •2H2O | 60 |  |  |
|  | pH 11-13 | NaOH |  |  | Prepare 3-6M solution, adjust to pH 11-13 |
|  | Current density - 50-500 A/m2 |  |  |  |  |
| 5c. Cu bath | Temp - 50 oC | CuSO4•5H2O | 35 |  |  |
| Option C | Time – 5-30min | NH4NO3 | 6 |  |  |
|  | pH 8-9 | K4P2O7 | 110 |  |  |
|  | Current density - 50-500 A/m2 | NaOH |  |  | Prepare 3-6M solution, adjust to pH 8-9 |
| 6. Porosity test | Temp - RT | K3Fe(CN)6 | 10 |  |  |
|  | Time – 20min | NaCl | 20 |  |  |

*Prepare those baths only if needed.

** prepare one of three possible etching baths accordingly to the electrode used.

- Experiment suggestion: comparison between electroless and electrodeposition.